	Table 1. Maximum endured load for the implant systems and the type of failure (38)

	
	Friad
XIVE
	Biomet
OSSEO
	NB Branemark
	NB Replace
	Zimmer TSV
	Stmn TL

	Maximum Endured Load [N]
	180
	200
	210
	220
	280
	480

	Fatigue Limit [N]
	203
	213
	220
	227
	306
	518

	Minimum fracture Load [N]
	200
	240
	250
	280
	320
	600

	Fracture Location
	Fracture of screw
	Fracture of implant
	Fracture of implant
	Fracture of implant
	Fracture of implant
	Fracture of implant






















	Table 2. Search strategies and the number of inputs used in the literature review in PubMed

	Date
	Search Equations
	Number of Articles

	1974–2024
	Dental implant system
	6024

	1992–2024
	Dental implant system, cyclic loading
	102

	2002–2024
	Dental implant system, cyclic loading, screw loosening
	19

	2011–2024
	Dental implant system, cyclic loading, implant complications
	3

	2011–2024
	Dental implant system, cyclic loading, screw loosening and implant complications
	2

	2022
	Dental implant system, cyclic loading, mechanical complications
	1

	2012–2024
	Dental implant system, cyclic loading, microleakage
	11






















	Table 3. Search strategies and the number of inputs used in the literature review in ScienceDirect.

	Date
	Search Equations
	Number of Articles

	2000–2024
	Dental implant system
	1786

	2001–2024
	Dental implant system, cyclic loading
	569

	2000–2024
	Dental implant system, cyclic loading, screw loosening
	85

	2000–2024
	Dental implant system, cyclic loading, implant complications
	257

	2000–2024
	Dental implant system, cyclic loading, screw loosening and implant complications
	58

	2004–2024
	Dental implant system, cyclic loading, mechanical complications
	90

	[bookmark: _GoBack]2022–2024
	Dental implant system, cyclic loading, microleakage
	14




